[image: image1.jpg]
    Product





    Type
XP0    
 
   

Synthetic Qualifying Oil
________________________________________________________________

XP0 Synthetic Racing Oil Product Information:

· For use in high powered, high performance race engines, including ASA, Late Model, Drag, etc.
· Uncompromised power, protection, performance.
· Used by Joe Gibbs Racing to qualify restrictor plate engines.
· Compatible with methanol and high octane race fuels.

· Recommended applications:
· NASCAR V-8 restrictor plate qualifying

· NHRA Pro Stock and Motorcycle engines
· 4 Cycle Go Kart engines with Babbitt type insert bearings
· Uses advanced, proprietary lubricant technology exclusive to Joe Gibbs Performance.
· Viscosity typical of SAE 0W.
Typical Physical Characteristics

	PARAMETER
	TEST METHOD
	VALUE

	Pounds per U.S. gallon at 15.6°C
	----
	6.86

	Specific Gravity at 15.6°C
	ASTM D1298
	0.824

	Viscosity at 40°C. cSt
	ASTM D445
	11.5

	Viscosity at 100°C, cSt
	ASTM D445
	3.3

	Flash Point (PMCC),°C
	ASTM D93
	149

	Pour Point, °C
	ASTM D97
	-54


* XP0 can be blended and is completely compatible with XP1, XP2 and XP3.
