[image: image1.jpg]



    Product





    Type
XP1     
  

 

Synthetic Racing Oil
________________________________________________________________

XP1 Synthetic Racing Oil Product Information:

· For use in high powered, high performance race engines, including ASA, Late Model, Drag, etc.
· Uncompromised power, protection, performance.
· Used in all Joe Gibbs unrestricted race engines (Nextel Cup, Busch and Late Model).
· Designed to handle 500 miles of competition, over 9500 rpm, and temperatures above 250 degrees.

· Exceptional performance in flat tappet race engines.

· Compatible with methanol and high octane race fuels.

· Recommended for:
·  Iron Block V-8 race engines with main and rod bearing clearances under 0.0025

· Flat-Tappet Race Engines

· Legends car engines

· Engines calling for 30 weight oil

· GM Crate Motors

· Uses advanced, proprietary lubricant technology exclusive to Joe Gibbs Performance.
· Viscosity typical of SAE 5W-20.
Typical Physical Characteristics

	PARAMETER
	TEST METHOD
	VALUE

	Pounds per U.S. gallon at 15.6°C
	----
	7.05

	Specific Gravity at 15.6°C
	ASTM D1298
	0.846

	Viscosity at 40°C. cSt
	ASTM D445
	50

	Viscosity at 100°C, cSt
	ASTM D445
	9.1

	Flash Point (PMCC),°C
	ASTM D93
	186

	Pour Point, °C
	ASTM D97
	-48


*XP1 can be blended and is completely compatible with XP2, XP3 and XP0.
