[image: image1.jpg]



    Product





    Type
XP2         Synthetic Restrictor Plate Racing Oil
________________________________________________________________

XP2 Synthetic Racing Oil Product Information:

· For use in high powered, high performance race engines, including ASA, Late Model, Drag, etc.
· Uncompromised power, protection, performance.
· Used in Joe Gibbs restrictor plate race engines (Nextel Cup, Busch and Late Model).
· Exceptional performance in flat tappet, restricted air intake race engines.

· Compatible with methanol and high octane race fuels.

· Recommended for:

· NASCAR V-8 restrictor plate race engines

· USAC Ford Focus Midgets

· Race engines with main and rod bearing clearances under .0020

· Uses advanced, proprietary lubricant technology exclusive to Joe Gibbs Performance.
· Viscosity typical of SAE 0W-20.
Typical Physical Characteristics

	PARAMETER
	TEST METHOD
	VALUE

	Pounds per U.S. gallon at 15.6°C
	----
	7.00

	Specific Gravity at 15.6°C
	ASTM D1298
	0.840

	Viscosity at 40°C. cSt
	ASTM D445
	31

	Viscosity at 100°C, cSt
	ASTM D445
	6.3

	Flash Point (PMCC),°C
	ASTM D93
	192

	Pour Point, °C
	ASTM D5985
	-54


* XP2 can be blended and is completely compatible with XP1, XP3, or XP0.
