[image: image1.jpg]



    Product





    Type
XP3     
   



Synthetic Racing Oil
________________________________________________________________

XP3 Synthetic Racing Oil Product Information:

· For use in aluminum blocks and looser clearance race engines.
· Outstanding high temperature-high shear protection.
· Compatible with methanol and high octane race fuels.

· Recommended for:
· Big Block dirt late model V-8 race engines 
· Sprint and midget race engines

· Turbo and supercharged  engines

· Ideal for wet sump engines and other race engines with main and rod bearing clearances over 0.0025
· Uses advanced, proprietary lubricant technology exclusive to Joe Gibbs Performance.
· Viscosity typical of SAE 10W-30.
Typical Physical Characteristics

	PARAMETER
	TEST METHOD
	VALUE

	Pounds per U.S. gallon at 15.6°C
	----
	7.08

	Specific Gravity at 15.6°C
	ASTM D1298
	0.850

	Viscosity at 40°C. cSt
	ASTM D445
	70

	Viscosity at 100°C, cSt
	ASTM D445
	12.0

	Flash Point (PMCC),°C
	ASTM D93
	189

	Pour Point, °C
	ASTM D97
	-54


* XP3 can be blended and is completely compatible with XP1, XP2 and XP0.
