[image: image1.jpg]



    Product





    Type
XP4     
   



Mineral Racing Oil
________________________________________________________________

XP4 Racing Oil Product Information:

· For use in high powered, high performance race engines.
· Uncompromised performance and protection for engines operating under severe, high contamination conditions 
· Designed for short duration racing where engine load and dirt and fuel contamination is high.
· Compatible with methanol and high octane race fuels.

· Recommended for:
· Big Block dirt late model V-8 race engines 
· Sprint and Midget Race Engines

· Race engines with main and rod bearing clearances over 0.0025
· Uses advanced, proprietary lubricant technology exclusive to Joe Gibbs Performance.
· Viscosity typical of SAE 15W-50.
Typical Physical Characteristics

	PARAMETER
	TEST METHOD
	VALUE

	Pounds per U.S. gallon at 15.6°C
	----
	7.36

	Specific Gravity at 15.6°C
	ASTM D1298
	0.884

	Viscosity at 40°C. cSt
	ASTM D445
	130

	Viscosity at 100°C, cSt
	ASTM D445
	17.1

	Flash Point (PMCC),°C
	ASTM D93
	178

	Pour Point, °C
	ASTM D97
	-12


