    Product





    Type

XP5     
   




Semi-Synthetic 








Racing Oil
________________________________________________________________

XP5 Semi-Synthetic Racing Oil Product Information:

· For use in gasoline powered, high performance race engines, including ASA, Late Model, Sprint, etc.
· A semi-synthetic oil based on our original formula race oil.
· Improved high temperature hear and oxidation stability compared to mineral oils.
· Viscosity typical of SAE 20W-50
Typical Physical Characteristics

	PARAMETER
	TEST METHOD
	VALUE

	Pounds per U.S. gallon at 15.6°C
	----
	7.26

	Specific Gravity at 15.6°C
	ASTM D1298
	0.872

	Viscosity at 40°C. cSt
	ASTM D445
	150

	Viscosity at 100°C, cSt
	ASTM D445
	17.7

	Viscosity Index
	ASTM D2270
	130

	Flash Point (PMCC),°C
	ASTM D93
	212

	Pour Point, °C
	ASTM D97
	-33


