    Product





    Type

XP6     
   



Synthetic Racing Oil
________________________________________________________________

XP6 Synthetic Racing Oil Product Information:

· For use in gasoline powered, high performance race engines, including ASA, Late Model, Sprint, etc.
· A full synthetic, SAE 15W-50 version of our race proven XP1 oil.
· Designed for aluminum blocks and looser clearances.

· Excellent bearing oil film thickness and outstanding cold start properties.
· Viscosity typical of SAE 15W-50
Typical Physical Characteristics

	PARAMETER
	TEST METHOD
	VALUE

	Pounds per U.S. gallon at 15.6°C
	----
	7.13

	Specific Gravity at 15.6°C
	ASTM D1298
	0.856

	Viscosity at 40°C. cSt
	ASTM D445
	113

	Viscosity at 100°C, cSt
	ASTM D445
	16.3

	Viscosity Index
	ASTM D2270
	155

	Flash Point (PMCC),°C
	ASTM D93
	149

	Pour Point, °C
	ASTM D97
	-39


